Introduction
The Industrial Automation High-Permeability Silicon Steel Motor Core is engineered to deliver superior magnetic performance and low iron loss, ensuring high-efficiency drive for modern industrial equipment. Constructed with premium silicon steel and laminated into 50–200 layers, this core minimizes eddy current loss and improves overall system stability.

Applications

Industrial automation lines: Precision robotic arms, conveyor drives, and automated valves.

High-precision control equipment: Systems requiring accurate torque and consistent output.

Energy-intensive machinery: Applications where efficiency and heat resistance are critical.

Key Advantages

High magnetic permeability for excellent magnetic flux and energy efficiency.

50–200-layer lamination significantly reduces eddy current and hysteresis loss.

Wide compatibility with DC and stepper motors.

Long service life even in demanding industrial environments.

Specification Table

| Parameter | Value |
| --- | --- |
| Material | High-permeability silicon steel |
| Core Thickness | 0.35–0.5 mm |
| Lamination Layers | 50–200 |
| Magnetic Permeability | 15,000–20,000 H/m |
| Operating Temperature | –20 °C to 120 °C |
| Applicable Motor Types | DC motor, stepper motor |

Production Process
High-grade silicon steel selection → Precision stamping and lamination → Core assembly with strict alignment → Heat treatment and insulation coating → Final electrical and magnetic testing for industrial automation standards.

After-Sales Service
One-year quality warranty with optional extended coverage, remote technical support, and rapid spare-parts supply to keep production lines running smoothly.

FAQ
Q1: Can the core handle continuous 24/7 operation?
A1: Yes, the lamination design ensures low heat rise for round-the-clock use.
Q2: Is customization available for different motor sizes?
A2: Yes, lamination layers and thickness can be tailored to specific requirements.